## Slide 1: Synthesis and Characterization of Eutectic High Entropy Alloys
By-
Yagyaval Singh Rajput (15120082)
Satyaki Chakravorty (15120065)
Pradeep Kumar (15120053)
Abhishek Paswan (15120003)
Under guidance of –
Dr Manoj Kumar Chopkar
Major Project Presentation for the partial fulfillment of the requirements of the B.Tech Degree
Department of Metallurgical Engineering
National Institute of Technology Raipur
December- 2018

## Slide 2
Outline
Introduction
Literature Review
Motivation and novelty statement
Objectives
Experimental Details
Future Works
References
Outline
Ph.D. Defence Seminar

## Slide 3
What is High Entropy Alloy ?
Multi-component alloys having constituents in equiatomic or near equiatomic ratios.
5-13 principal elements (atomic concentration 5% to 30%)
High softening resistance elevated temperatures & sluggish diffusion kinetics
Low-Entropy Alloys
ΔSconf ≤ R
Medium Entropy Alloys
R≤ΔSconf≤1.5R
High Entropy Alloys
ΔSconf≥1.5R
Fig. 1 Alloy world based on configurational entropy(1)

## Slide 4
How High Entropy Alloy?
Ph.D. Defence Seminar
High Entropy Alloys
(Structure) Lattice Distortion Effect
(Kinetics)
Sluggish Diffusion Effect
Cocktail Effect
(Thermodynamics)
High Entropy Effect
The Coring effect(3)

## Slide 5
ARC MELTING
Ph.D. Defence Seminar
MECHANICAL ALLOYING
Synthesis and Processing of HEA System
SPUTTERING
LASER CLADDING & ELECTRO-DEPOSITION

## Slide 6
Why High Entropy Alloy?
Major Advantages
Single phase FCC –Ductile
Single phase BCC – High yield strength
High wear resistance
High corrosion resistance
Major Disadvantages
Difficult to achieve a reasonable balance between strength & ductility
Inferior cast-ability and compositional segregation
Ph.D. Defence Seminar

## Slide 7
Eutectic High Entropy Alloy
A mixture of soft fcc and hard bcc phases, to achieve the balance of high fracture strength and high ductility.
A good candidate high temperature alloys, because the eutectic solidification structure
  has the following features :-
  near-equilibrium & controllable microstructures
  low-energy phase boundaries
  high yield strength
  good high-temperature creep resistance
  regular lamellar or rod-like eutectic organization
  better castability
Ph.D. Defence Seminar

## Slide 8
Proposed Applications
Engine materials (4,5,6)
-Better elevated-temperature strength
-Oxidation resistance
-Hot corrosion resistance
Light transportation materials
-Strength
-Toughness
-Workability
Functional coatings materials
-Better wear resistance
Ph.D. Defence Seminar

## Slide 9
Literature Review
Ph.D. Defence Seminar
Designing of EHEA’s
Two main methods :-
Calculation of phase diagrams (CALPHAD) method(2)
Experimental Method
Neither of above can be adopted due to :-
Guidelines assumptions
Complexity & inaccuracy of multi-component phase diagrams
Inaccuracy of experimental determination
Solution ???
Pseudo Binary alloy system

## Slide 10
Literature Review
Ph.D. Defence Seminar
One Component
  Three stable FCC-structured HEAs (CrFeCoNi2, CrFeCo2Ni, CrFe2CoNi)
Intermetallic compound(2)
  With subject to conditions :-
The single-phase solid solution should be stable enough without element segregation and precipitated phase.
IMC should be stable enough from room temperature to its melting point
IMC must have the most negative enthalpy
Avoid the formation of other IMCs.
Pseudo Binary Alloy System

## Slide 11
Literature Review
Ph.D. Defence Seminar
Designing of pseudo binary EHEA’s with FCC & BCC dual phases using thermodynamic parameters also(7,8)
Enthalpy Mix
  Solid solution will form when -5KJ/mol<△Hmix<+5KJ/mol(8)
Valance electron Concentration
  BCC phase will be stable when VEC<6.87
  FCC phase will exist when VEC>8
  BCC/FCC Dual phases will co-exist when 6.87 <VEC< 8
Design strategy :-

## Slide 12
Motivation of The Present Work
Previously, study carried out on the Cr-Cu-Fe-Co-Ni-Si
Cr-Cu-Fe-Co-Ni2-Si and Cr-Cu-Fe2-Co-Ni2.1-Si0.55 high entropy alloys.
Literature review on Cr-Cu-Fe-Co-Ni-Si, Cr-Cu-Fe-Co-Ni2-Si and Cr-Cu-Fe2-Co-Ni2.1-Si0.55 HEAs suggests that addition of external elements is favorable for the changes in the microstructural and mechanical properties.
Researchers ignored the addition of non-metallic elements such as Si and focused only to regulate metallic elements for eutectic phase formation and mechanical properties improvement.
A simple and practicable method was proposed to design pseudo binary EHEAs
  composed of FCC/B2 dual phases.
Ph.D. Defence Seminar

## Slide 13
Objectives of the Present Study
To prepare three EHEA’s containing elements CoCrCuFeNiSi by vacuum arc melting.
To investigate the effect of silicon (Si) and nickel(Ni) addition on the
  phase evolution, mechanical properties (Hardness and Wear) and corrosion behavior.
To investigate the effect of processing route on phase evolution, mechanical properties (Hardness and Wear) and corrosion behavior.
Ph.D. Defence Seminar

## Slide 14
Methodology
Fig. The flow chart showing the steps followed for the characterization of EHEAs prepared by arc melting route.
Procurement of Elemental Powders
Arc Melting
Characterization of Phase Evolution
(XRD, SEM and EDS)
Characterization of Physical Properties
(Hardness and Corrosion Behavior)
Results/Data Analysis
Summary and Conclusion
Consolidation
Ph.D. Defence Seminar

## Slide 15
Compositional Details
Ph.D. Defence Seminar
Cr-Cu-Fe-Co-Ni-Si
Cr-Cu-Fe-Co-Ni2-Si
Cr-Cu-Fe2-Co-Ni2.1-Si0.55
Elements | Cr | Cu | Fe | Co | Ni | Si
Atomic Wt. % | 16.395 | 20 | 17.6 | 18.55 | 18.5 | 8.85
Elements | Cr | Cu | Fe | Co | Ni | Si
Atomic Wt. % | 13.8 | 16.9 | 14.85 | 15.65 | 31.2 | 7.45
Elements | Cr | Cu | Fe | Co | Ni | Si
Atomic Wt. % | 14.05 | 17.2 | 15.1 | 15.95 | 33.395 | 4.15
1. Mixing & Weighing
The elemental powders of Co, Cu, Cr, Fe, Ni and Si were used as starting material to synthesize EHEAs
Each compositions was weighed in a total of 20 grams

## Slide 16
Experimental
2. Consolidation
Ph.D. Defence Seminar
3. Arc-Melting
Melting chamber
Casting chamber
Electrodes
Pressure gauge
Final product
Arc melting in a water-cooled copper hearth under
Argon atmosphere.
The arc-melted buttons were flipped and re-melted at least five times to promote thorough mixing
Compaction pressure is 4000psi
Die size 20mm

## Slide 17
Experimental
3. Polishing & Etching
Polishing
Belt Grinder
Paper Polishing (SiC Paper)
  200
  400
  600
  1000
  2000
Alumina Cloth Polishing
Etching
Copper Etchant
FeCl3 – 5g
HCl – 5ml
Ethanol – 50ml
Distilled water – 50ml
Ph.D. Defence Seminar

## Slide 18
Experimental
Optical
Microstructures
  100x
Ph.D. Defence Seminar
Cr-Cu-Fe-Co-Ni2-Si
Cr-Cu-Fe-Co-Ni-Si
Cr-Cu-Fe-Co-Ni2.1-Si0.55

## Slide 19
Experimental
Ph.D. Defence Seminar
Cr-Cu-Fe-Co-Ni-Si
Cr-Cu-Fe-Co-Ni2-Si
Cr-Cu-Fe-Co-Ni2.1-Si0.55
Scanning Electron Microscopy (SEM)

## Slide 20
Experimental
XRD Data
Ph.D. Defence Seminar
● FCC
Ni3Si

## Slide 21
EDX
Ph.D. Defence Seminar

## Slide 22
Micro-Hardness
Ph.D. Defence Seminar
Chart: 
| CrCuFeCoNi2.1Si0.55 | CrCuFeCoNi2Si | CrCuFeCoNiSi
MICRO HARDNESS VALUES(AVG) | 318 | 345 | 391

## Slide 23
Comparision
Ph.D. Defence Seminar
XRD comparison with base HEA
CoCrCuFeNi

## Slide 24
Comparision
Ph.D. Defence Seminar
Chart: 
| CrCuFeCoNi | CrCuFeCoNi2.1Si0.55 | CrCuFeCoNi2Si | CrCuFeCoNiSi | 316 Stainless Steel | Ti-6Al-4V
MICRO HARDNESS VALUES(AVG) | 286 | 318 | 345 | 391 | 186 | 412
Hardness comparison with base HEA & others

## Slide 25
References
[1]J.W. Yeh, S.K. Chen, S.J. Lin, J.Y. Gan, T.S. Chin, T.T. Shun, C.H. Tsau, S.Y. Chang, Adv. Eng. Mater. 6 (2004) 299–303+274.
[2] Xi Jina, Yang Zhoua, Lu Zhanga, Xingyu Dua, Bangsheng Lia,b* 633–648.
[3]C.-J. Tong, Y.-L. Chen, J.-W. Yeh, S.-J. Lin, S.-K. Chen, T.-T. Shun, C.-H. Tsau, S.-Y. Chang, Metall. Mater. Trans. A 36 (2005) 881–893.
[4]A. Takeuchi, N. Chen, T. Wada, Y. Yokoyama, H. Kato, A. Inoue, J.W. Yeh, Intermetallics 19 (2011) 1546–1554.
[5]Z. Liu, S. Guo, X. Liu, J. Ye, Y. Yang, X.L. Wang, L. Yang, K. An, C.T. Liu, Scr. Mater. 64 (2011) 868–871.
[6] F. Otto, Y. Yang, H. Bei, E. P. George. Relative effects of enthalpy and entropy on
the phase stability of equiatomic high-entropy alloys, Acta Mater. 61 (2013)
2628-2638.
[7] D. B. Miracle, O. N. Senkov. A critical review of high entropy alloys and related
concepts, Acta Mater. 122 (2016) 448-511.
[8] Y. P. Lu, Y. Dong, S. Guo, L. Jiang, H. J. Kang, T. M. Wang, B. Wen, Z. J. Wang, J.
C. Jie, Z. Q. Cao, H. H Ruan, T. J. Li. A Promising New Class of High-Temperature
Alloys: Eutectic High-Entropy Alloys, Sci. Rep. 4 (2014) 6200.
Ph.D. Defence Seminar

## Slide 26: Thank you
.

## Slide 27
XRD Analysis
Ph.D. Defence Seminar
● FCC
Ni3Si
Cr-Cu-Fe-Co-Ni-Si
Cr-Cu-Fe-Co-Ni2-Si
Cr-Cu-Fe-Co-Ni2.1-Si0.55

## Slide 28
Future Works
SEM(Scanning Electron Microscopy)
EDS analysis(Electron Dispersive Spectrometry)
DSC analysis(Differential Scanning Calorimetry)
Corrosion Test
Hardness Test
Wear Resistance Test
Ph.D. Defence Seminar